April 22, 2013 Irradiation Report

- Description of the experiment:

Picture of the jar.

Picture of the jar.

- The experiment was done on 22/4/2013. Irradiation started at 11:19 am, and stopped at 12:19 pm.

- The beam parameters were as the following:

- Energy of electron beam was 41MeV.

- Maximum Current was 65mA.

- Rep Rate was 41 Hz.

- Pulse width was 9 microseconds.

- Power of beam found from calculation (983 watt).

- Nickel Foils were two pieces described as the following:

- Nickel (1)

It was in front of the stack. It was counted on April 22,2013. Counting started at 16:53:44 and stopped at 17:04:41.

- Nickel (2)

It was in the back of the stack. It was counted on April 22,2013. Counting started at 16:41:30 and stopped at 16:52:43.

- The reaction is [Ni-58 (, n) Ni-57].

- The measurement was done in position K. The gamma line used for measurement was 1378 KeV and corresponding detector efficiency for this energy and position was 0.0003227 .The half live of Ni-57 is 36 hours.

- The activities were found to be:

Picture of the silver coins and Ni foils before Irradiation.

Picture of the silver coins and Ni foils before Irradiation.

| Foils | Masses ‘g’ | Activity |
| --- | --- | --- |
| Ni (1) | 0.153 | 2.949 |
| Ni (2) | 0.161 | 2.582 |

Table (1): Activities were found for Ni foils.

Table (1): Activities were found for Ni foils.

- Detection Limits

The detection limit was calculated by this equation,.

Where: Concentration. : Standard Deviation. Y: yield “total count”.

Table (2): Description of Detection limit for Ni foils.

| Isotopes | Concentration | Standard Deviation | Yield “Count” | Detection limit |
| --- | --- | --- | --- | --- |
| Ni (1) | 153.8 mg | 4.788 | 16803 counts | 0.0876 |
| Ni (2) | 161.5 mg | 3.528 | 15040 counts | 0.0757 |

Counts

Counts

Energy (KeV)

Energy (KeV)

Figure 2: Gamma spectrum of Ni-57 emission

Figure 2: Gamma spectrum of Ni-57 emission

- Silvers coins were three pieces described as the following:

- The big Coin was counted on April 22, 2013 from 17:07:34 till 17:19:17.

- The medium Coin was counted on April 22, 2013 from 17:20:50till 17:37:18.

- The Small Coin was counted on April 22, 2013 from 17:38:29 till 17:53:09.

- The measurement was done in position N.

- The following reaction were observed in silvers coins :

- [Ag-107 (γ, n) Ag-106m]

- [Ag-107 (γ, 2n) Ag-105]

| Coins | Masses ‘g’ |
| --- | --- |
| Big | 6.8921 |
| Medium | 4.6280 |
| Small | 6.9325 |

Table (3): Masses of silver coins

Table (3): Masses of silver coins

Picture of the silver coins after Irradiation.

Picture of the silver coins after Irradiation.

- The activities for each Isotopes

| Small coin [Ag-106m] |  |
| --- | --- |
| Energy ‘KeV’ | Efficiency | Half live ‘d’ | Activity |
| 451 | 0.00017397 | 8.3 | 4.2235 |
| 429.64 | 0.00013036 | 8.3 | 4.2036 |
| 616.17 | 0.00013765 | 8.3 | 4.2123 |
| 717 | 0.00012285 | 8.3 | 3.9925 |
| 748.44 | 0.00011889 | 8.3 | 4.0778 |
| 804.34 | 0.00011259 | 8.3 | 3.7550 |
| 1046 | 0.00009231 | 8.3 | 3.7793 |
| The Average of activities = 4.034±0.2011 |  |

Table (4): Description of Activities for Ag-106m from the small coin.

| Medium coin [Ag-106m] |
| --- |
| Energy ‘KeV’ | Efficiency | Half live ‘d’ | Activity |
| 451 | 0.00017397 | 8.3 | 2.8919 |
| 429.64 | 0.00013036 | 8.3 | 2.8555 |
| 616.17 | 0.00013765 | 8.3 | 2.9342 |
| 717 | 0.00012285 | 8.3 | 2.8755 |
| 748.44 | 0.00011889 | 8.3 | 2.9762 |
| 804.34 | 0.00011259 | 8.3 | 2.7415 |
| 1046 | 0.00009231 | 8.3 | 2.5455 |
| The average of activities = 2.8314±0.1457 |

Table (5): Description of Activities for Ag-106m from medium coin.

| Big coin [Ag-106m] |
| --- |
| Energy ‘KeV; | Efficiency | Half live ‘d’ | Activity |
| 451 | 0.00017397 | 8.3 | 4.1787 |
| 429.64 | 0.00013036 | 8.3 | 4.0979 |
| 616.17 | 0.00013765 | 8.3 | 4.2499 |
| 717 | 0.00012285 | 8.3 | 3.9189 |
| 748.44 | 0.00011889 | 8.3 | 4.1904 |
| 804.34 | 0.00011259 | 8.3 | 3.9159 |
| 1046 | 0.00009231 | 8.3 | 3.7054 |
| The average of activities = 4.0367±0.1963 |

Table (6): Description of Activities for Ag-106m from big coin.

|  | Small coin [Ag-105] |
| --- | --- |
| Energy ‘ KeV’ | Efficiency | Half live | Activity |
| 280 | 0.0002458 | 41.2 | 2.0825 |
| 345 | 0.0002119 | 41.2 | 2.3032 |
| 443 | 0.0001763 | 41.2 | 2.0809 |

Table (7): Description of Activities for Ag-105 from small coin.

Table (8): Description of Activities for Ag-105 from big coin.

Table (8): Description of Activities for Ag-105 from big coin.

| Big coin [Ag-105] |
| --- |
| Energy ‘KeV’ | Efficiency | Half live ‘d’ | Activity |
| 280 | 0.0002458 | 41.2 | 1.8874 |
| 345 | 0.0002119 | 41.2 | 2.4083 |
| 443 | 0.0001763 | 41.2 | 2.3121 |
| Medium coin [Ag-105] |
| Energy ‘KeV’ | Efficiency | Half live ‘d’ | Activity |
| 280 | 0.0002458 | 41.2 | 1.4322 |
| 345 | 0.0002119 | 41.2 | 1.5998 |
| 443 | 0.0001763 | 41.2 | 1.5961 |

Table (9): Description of Activities for Ag-105 from medium coin.

Table (9): Description of Activities for Ag-105 from medium coin.

Counts

Counts

Energy (KeV)

Energy (KeV)

Figure 3: Gamma spectrum of Ag-106m emission

Figure 3: Gamma spectrum of Ag-106m emission

…………………………………………………………………………………………………………………………………………………

5) Slag